CONCLUSION

Estimation of heat fluxes and surface temperature values attained by space vehicles during atmospheric reentry is essential for a fail-safe reentry. Hence, we evaluated the emissivity and catalycity efficiency of the materials used in aerospace applications. We aimed to design and then utilize materials having high emissivity and low catalycity efficiency. In this study, we have illustrated the measurement of hemispherical emissivity and atomic recombination coefficients of C/SiC composites that can be applied to the TPS of spacecrafts.

Using the MEDIASE facility, we tested the C/SiC samples within a temperature range of 950–1900 K and at both 4 Pa and 200 Pa; the samples exhibited relatively high emissivity values of approximately 0.7. This result confirms that the glassy oxide layer greatly determines the radiative behavior of SiC-coated C/SiCs. By contrast, in the MESOX facility, the catalycity measurements demonstrated a low oxygen recombination coefficient at high temperature (~0.07 at 1800 K). The tests have also demonstrated strong dependence of the recombination coefficient on surface morphology, which varies only slightly among samples because of manufacturing concerns. Whereas samples from the same production batch have shown different recombination coefficient values, the general catalycity trend remains the same. This characteristic enables evaluation of the activation energy of atomic oxygen recombination (~30 KJ/mol).

Our results substantiate the suitability of a C/Sic application in hot structures for reentry vehicles. However, strategic manufacturing process control for C/SiC production to obtain specific morphology of samples would further ascertain defined emissivity and catalycity values.

# Comments

Remark: Note that this information has already been mentioned in the Introduction section and may not be repeated here. Hence, we have deleted it; please check.

Language:

The author has been informed about the nature and relevance of revision made here through a remark.

Language:

The redundancy has been eliminated.

Language:

The phrase has been made concise.

Subject area:

A precise technical phrase has replaced the wordy expression.

Language & typographical error:

To achieve fluency, the phrase has been restructured and the spelling error has been corrected.

Language:

The sentence has been reframed for a robust expression and author stance.

Language:

The phrasal verb has been replaced with an academic word choice for accuracy and conciseness.

Style:

The abbreviation has already been defined earlier in the text.

Language:

The sentence has been restructured to enhance readability.

Content accuracy:

Crucial information has been corrected as per the study.

Language:

The awkward word order has been corrected.

Attention to detail:

Placing a semicolon here has made the sentence readable.

Language:

Technical writing calls for a discipline-specific academic vocabulary, and hence the original has been replaced with formal academic language.

Style:

The revised spelling conforms to American English convention.

Language:

The content has been made readable and clear.

Language:

The lengthy noun string has been rephrased for clarity and readability.

Language:

The sentence has been restructured to cohere with the context and redundancy has been eliminated.

Language:

The information in this sentence contrasts that of the preceding one. Hence, an appropriate transition word has been added.

Remark: The limitation(s) of the experiment has not been stated in the manuscript. Please mention any constraints observed during the experimental phase in this section. This sentence will therefore have a reference point for the reader.

Language:

Through a remark, the author is informed of content that needs to be corroborated and presented.