CONCLUSION

Estimation of heat fluxes and surface temperature values attained by spacecraft vehicles during atmospheric reentry is essential for a reentry without any mechanical and physical problems. Hence, we evaluated the emissivity and catalycity efficiency of the materials used in aerospace applications. We aimed to design and then utilize materials having high emissivity and low catalycity efficiency. In this paper, we have illustrated the measurement of hemispherical emissivity and atomic recombination coefficients of C/SiC composites. These composites find suitable application in the TPS of spacecrafts.

Using the MEDIASE facility, we tested the C/SiC samples within a temperature range of 950–1900 K and at both 4 Pa and 200 Pa; the samples exhibited relatively high emissivity values of approximately 0.7. This result confirms that the glassy oxide layer greatly determines the radiative behavior of SiC-coated C/SiCs. By contrast, in the MESOX facility, the catalycity measurements demonstrated a low oxygen recombination coefficient at high temperature (~0.07 at 1800 K). The tests have also demonstrated strong dependence of the recombination coefficient on surface morphology, which varies only slightly among samples because of manufacturing concerns. Whereas samples from the same production batch have shown different recombination coefficient values, the general catalycity trend remains the same. This characteristic enables evaluation of the activation energy of atomic oxygen recombination (~30 kJ/mol).

Our results substantiate the suitability of a C/SiC application in hot structures for atmospheric reentry vehicles. However, strategic manufacturing process control for C/SiC production to obtain specific types of samples would further ascertain defined emissivity and catalytic values.

# Comments

Language:

The phrase has been made concise.

Punctuation:

The comma sets off the introductory adverb from the rest of the sentence.

Typographical error:

The spelling has been corrected.

Word choice:

The phrasal verb has been replaced with an academic word choice for accuracy and conciseness.

Style:

The abbreviation has already been defined earlier in the text.

Grammar:

The singular noun has been used here for factual correctness.

Punctuation:

An en dash denotes a range between values.

Attention to Detail:

A space has been added between the unit and value. This revision has been made throughout the manuscript.

Language:

The awkward word order has been corrected.

Grammar:

The run-on sentence has been corrected by adding the right punctuation.

Style:

The spelling has been changed according to the American convention.

Punctuation:

Comma added here for the introductory prepositional phrase

Grammar:

The adverb placement has been revised for readability.

Grammar:

The verb has been made plural to match the plural subject “samples”.

Grammar:

The tense has been corrected within context.

Grammar:

The definite article “the” is required here as the “of”-phrase makes the noun “energy” specific.

Grammar:

The article is not needed here as the noun “structures” is generic.

Grammar:

The preposition has been corrected.

Punctuation:

The period has replaced the ellipses.