CONCLUSION

Estimation of heat fluxes and surface temperature values attained by space vehicles during atmospheric reentry is essential for a fail-safe reentry. Hence, we evaluated the emissivity and catalycity efficiency of the materials used in aerospace applications. We aimed to design and then utilize materials having high emissivity and low catalycity efficiency. In this study, we have illustrated the measurement of hemispherical emissivity and atomic recombination coefficients of C/SiC composites that can be applied to the TPS of spacecrafts.

Using the MEDIASE facility, we tested the C/SiC samples within a temperature range of 950–1900 K and at both 4 Pa and 200 Pa; the samples exhibited relatively high emissivity values of approximately 0.7. This result confirms that the glassy oxide layer greatly determines the radiative behavior of SiC-coated C/SiCs. By contrast, in the MESOX facility, the catalycity measurements demonstrated a low oxygen recombination coefficient at high temperature (~0.07 at 1800 K). The tests have also demonstrated strong dependence of the recombination coefficient on surface morphology, which varies only slightly among samples because of manufacturing concerns. Whereas samples from the same production batch have shown different recombination coefficient values, the general catalycity trend remains the same. This characteristic enables evaluation of the activation energy of atomic oxygen recombination (~30 kJ/mol).

Our results substantiate the suitability of a C/Sic application in hot structures for reentry vehicles. However, strategic manufacturing process control for C/SiC production to obtain a specific morphology of samples would further ascertain defined emissivity and catalycity values.

# Comments

Grammar:

Based on the given context and for consistency, the countable form of the noun has been used.

Language:

The redundancy has been eliminated.

Language:

The phrase has been made concise.

Language:

A better word choice has replaced the original for conciseness.

Subject-specific word choice:

A precise technical phrase has replaced the wordy expression.

Clarity & typographical error:

To achieve fluency, the phrase has been restructured and the spelling error corrected.

Language:

The sentence has been reframed for a robust expression and author stance.

Word choice:

The phrasal verb has been replaced with an academic word choice for accuracy and conciseness.

Style:

The abbreviation has already been defined earlier in the text.

Language:

The sentence has been restructured to enhance readability.

Grammar:

The study used different samples; the noun has been pluralized.

Language:

The awkward word order has been corrected.

Punctuation:

Placing a semicolon here has made the sentence readable.

Word choice:

Technical writing calls for a discipline-specific academic vocabulary, and hence the original has been replaced with formal academic language.

Technical word choice:

The correct technical word has been inserted here.

Style:

The revised spelling conforms to American English convention.

Typographical error:

The spelling error has been corrected.

Language:

The wordy phrase has been made concise.

Language:

The sentence has been restructured to cohere with the context, and redundancy has been eliminated.